The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

A high resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at https://www.masterbond.com/newsrelease/ep42-2lv-black

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

NASA Low Outgassing Rated Epoxy Features Enhanced Chemical Resistance

EP42-2LV Black is a two part epoxy with low viscosity and good flow. It withstands prolonged immersion in many acids, bases, solvents, fuels and oils. This versatile system can be used for bonding, sealing, coating and casting, where a strong chemical resistance profile is required.

This compound has an easy to use mix ratio of 100 to 40 by weight or 100 to 50 by volume with Part A being black and Part B being light amber. The viscosity of the mixed system is around 1,000-2,000 cps, and it has a long working life of 60 to 90 minutes per 100 gram batch. EP42-2LV Black cures optically opaque at room temperature in 2 to 3 days or at elevated temperatures of 200°F in 2 to 3 hours. For optimal performance, the recommended cure schedule is overnight at room temperature followed by heat curing at 150-200°F for 2 to 4 hours.

It meets NASA low outgassing specifications and is serviceable over a wide temperature range from -60°F to 350°F. This system is electrically insulative with a volume resistivity greater than 1014 ohm-cm and a dielectric constant of 4.0 at 60 Hz, at room temperature. These attributes, combined with its relatively long working life and lower exotherm, make EP42-2LV Black suitable for many larger potting and encapsulation applications.

EP42-2LV Black is recommended for applications in aerospace, electronic, optical and OEM industries. It is available in 1/2 pint, pint, quart, and gallon kits. Specialty packaging is also available in gun dispensers and premixed and frozen syringes.

Master Bond Chemically Resistant Adhesives

Master Bond EP42-2LV Black is a two component, low viscosity epoxy system that offers chemical resistance to a wide range of bases and solvents. Read more about Master Bond’s chemically resistant adhesives at https://www.masterbond.com/properties/chemical-resistance or contact technical support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: https://www.masterbond.com/tds/ep42-2lv-black

Check out new videos on our YouTube channel: https://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #