-----------------------------------------------------------------

The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

A high resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at https://www.masterbond.com/newsrelease/supreme-17htnd-2

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Toughened, One Component Epoxy Features High Glass Transition Temperature

Master Bond Supreme 17HTND-2 is a toughened epoxy system for bonding and sealing applications. It is a true one component system, not premixed and frozen, with an unlimited working life at room temperature. Supreme 17HTND-2 is thermally stable, featuring a high glass transition temperature (Tg) of 410°F (210°C). It also meets NASA low outgassing specifications per ASTM E595 testing.

Supreme 17HTND-2 has reliable electrical insulation properties with a volume resistivity exceeding 1015 ohm-cm at 75 °F. It possesses high bond strength properties with a lap shear strength of 1,900-2,100 psi and a tensile strength of 7,000-8,000 psi. It is designed to withstand thermal cycling and offers a wide service temperature range from -100°F to +550°F (-73°C to 288°C). Along with its simple handling properties, it has a paste consistency and is completely non-drip, making it ideal for applications where no flow is critical.

Supreme 17HTND-2 cures at elevated temperatures with cure schedule options including 300°F for 4-6 hours or 350°F for 2-4 hours. An optimal cure schedule is at 300°F for 4-6 hours, followed by a post cure at 350°F for 8-12 hours. It bonds well to a wide variety of substrates including metal, ceramics, composites and several plastics. Black in color, it is available in standard packaging of jars and cans, ranging from ½ pint to gallon containers.

Master Bond Toughened Epoxy Systems

Supreme 17HTND-2 is a high strength, toughened epoxy adhesive ideal for applications that require resistance to high temperatures as well as thermal cycling. Read more about Master Bond’s and toughened adhesive systems at https://www.masterbond.com/properties/flexibilized-and-toughened-adhesive-systems or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: https://www.masterbond.com/newsrelease/supreme-17htnd-2

Check out new videos on our YouTube channel: https://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #