-----------------------------------------------------------------

The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

A high resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at https://www.masterbond.com/newsrelease/uv15rcl.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

One Part Epoxy Changes from Red to Clear Under UV Light

Master Bond UV15RCL is a low viscosity, cationic type UV curing system with a special color changing feature. The originally red material changes to clear once exposed to UV light; indicating that there is UV light access across the adhesive material. Although this change in color from red to clear does not indicate a full cure it does confirm that the UV light has reached the polymer. By giving immediate visual feedback UV15RCL offers processing and handling advantages over conventional systems. Curing under UV light typically takes 30-60 seconds with a broad-spectrum UV lamp emitting light with a wavelength range between 320-365 nm. The minimum energy required is 20-40 milliwatts per cm².

UV15RCL features a high glass transition temperature (Tg) of 90-95°C. However, when post cured for 1-2 hours at 125°C, the Tg can increase to 125-130°C. It has a service temperature range from -80°F to +350°F. This non-solvent based system cures tack free and has a very low viscosity of 115-350 cps, making it ideal for spin coating. It is not oxygen inhibited and provides light transmission properties and good optical clarity, with a refractive index of 1.517. Also, it is an excellent electrical insulator with a volume resistivity exceeding 1014 ohm-cm.

UV15RCL is suitable for bonding and sealing applications as it adheres well to metals, glass, ceramics and many plastics, including acrylics and polycarbonates.  It is available in a wide range of packaging options, including syringes, ½ pint, pint, quart and gallon containers.

Master Bond UV Curing Adhesive Systems

Master Bond’s UV curing product line features ultra-fast curing compounds ideal for various bonding, sealing and coating applications in the aerospace, medical, electronic, and optical industries. Read more at https://www.masterbond.com/products/uv-curable-systems or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: https://www.masterbond.com/tds/uv15rcl

Video to see UV15RCL in action: https://youtu.be/3PSv60n3sRg

Check out more videos on our YouTube channel: https://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #