This email was sent to (%email%)

Unsubscribe at: http://www.masterbond.com/phplist/?p=unsubscribe&id=2

Subscribe at: http://www.masterbond.com/phplist/?p=subscribe&id=2

----------------------------------

The following is a news release from Master Bond Inc.  You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution versions of this image and files with the body text of this release are available at http://www.masterbond.com/mbnr.html?nr=ep13.

----------------------------------

FOR IMMEDIATE RELEASE

One Part Epoxy Adhesive

Resists High Temperatures

HACKENSACK, NJ - Nov 6, 2008 – Master Bond Inc., Hackensack, N.J. has introduced a new single component, high performance epoxy adhesive called EP13.  This compound requires no mixing and has an unlimited working life at room temperature.  EP13 has excellent bond strength to similar and dissimilar substrates and superior dimensional stability.  It has a service operating temperature range of -60°F to 450°F.

Master Bond EP13 is 100% reactive and does not contain any solvents or diluents.  It can be applied to vertical surfaces without sagging or dripping.  It cures at temperatures of 300°F to 350°F for 60-90 minutes.  The higher the temperature the faster the cure speed.

EP13 possesses high compressive strength and is readily machinable.  Upon cure, EP13 readily obtains tensile shear strengths in excess of 3,500 psi.  Resistance to a wide range of chemicals including fuels, acids, bases, oils and many solvents is exceptional.  EP13 has low shrinkage upon cure and good electrical insulation properties.  The standard color is grey.

Master Bond EP13 is available in pint, quart, gallon and 5 gallon containers.

CONTACT:

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: 201-343-8983

Fax: 201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ  07601-3922

Web: www.masterbond.com

# # #