This email was sent to (%email%)

Unsubscribe at: http://www.masterbond.com/phplist/?p=unsubscribe&id=2

Subscribe at: http://www.masterbond.com/phplist/?p=subscribe&id=2

----------------------------------

The following is a news release from Master Bond Inc.  You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution versions of this image and files with the body text of this release are available at http://www.masterbond.com/mbnr.html?nr=uv10tk40.

----------------------------------

FOR IMMEDIATE RELEASE

UV Curable Compound With

Superior Gap Filling Properties

HACKENSACK, NJ – Oct 29, 2009 – Master Bond UV10TK40 is a UV curable, no-mix epoxy resin system with exceptional sealing and gap-filling properties.  It excels in applications such as aligning parts and bonding irregularly shaped surfaces, especially in production environments where increased speed and reduced waste are paramount.  Its very high surface hardness (Shore A >75) also makes it an excellent choice for clear coating.

UV10TK40 is easy to apply and has a viscosity of 35,000 – 45,000 cps.  In addition to our standard packaging, UV10TK40 is also available in convenient, ready-to-use syringe applicators.  The system contains no solvents or other volatiles and is 100% reactive.

UV10TK40 is not oxygen inhibited and cures rapidly in the presence of air upon exposure to UV light at room temperatures.  It forms highly durable bonds with a typical tensile strength of 8,300 psi, a Young’s modulus of 245,000 psi, and an elongation at break of 6%.  Additionally, it has good dimensional stability and high heat stability (94°C Tg).

CONTACT:

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: 201-343-8983

Fax: 201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ  07601-3922

Web: www.masterbond.com

# # #